Physical Properties for Tempered Premium Hardboard

Manufacturing Specifications

For additional information contact Ampersand at 1-800-822-1939

1/8" Tempered Premium Hardboard

| Property | Minimum/Maximum |  | Average Value |  |
| --- | --- | --- | --- | --- |
| Thickness | 0.105”-0.135” |  | 0.118” |
| Modulus of Rupture (MOR) | ≥5500 psi |  | 6500 psi |
| Internal Bond (PTS) | ≥80 psi |  | 120 psi |
| 24 hr. Thickness Increase (TI) | ≤35% |  | 28% |
| Density (lbs./ft^3) |  | 65 |  |
| Moisture Content |  | 3-5% |  |
| Formaldehyde Emissions 1 |  | <.03 ppm |  |

1/4" Tempered Premium Hardboard

| Property | Minimum/Maximum |  | Average Value |
| --- | --- | --- | --- |
| Thickness | 0.205”-0.235” |  | 0.218” |
| Modulus of Rupture (MOR) | ≥4300 psi |  | 4500 psi |
| Internal Bond (PTS) | ≥70 psi |  | 90 psi |
| 24 hr. Thickness Increase (TI) | ≤30% |  | 20% |
| Density (lbs./ft^3) |  | 54 |  |
| Moisture Content |  | 3-5% |  |
| Formaldehyde Emissions 1 |  | <.03 ppm |  |

Footnotes: 1: NAUF (No Added Urea Formaldehyde) manufacturing process means products are exempt from/automatically comply with CARB regulations for indoor air quality.

Fabrication accuracy is generally stated as the length and width dimension of +0”, -1/16”.

All tests are conducted using guidelines in ASTM D 1037